## Slide 1: 5. Elasticity
Dr. Dawn Shuttle, PEng
Mike Jefferies, PEng
January, 2015

## Slide 2: Elasticity
Slight detour required – as we do not have time to calibrate elasticity in this workshop………..
BUT – elasticity is important.
ELASTICITY
    This is the small strain value – “Gmax”
    Forget strain-dependent elasticity as this doesn’t exist.
    “Measured” by bender elements in the lab
    “Measured” by the seismic CPT in the field

## Slide 3: Measuring shear modulus: “Gmax”
Elastic wave theory: G = r Vs2
Vs = Range / DTime
Tame seismic source
P-wave arrival
S-wave arrival
Whacking left
Whacking right
Source geophone
Downhole
geophone

## Slide 4: Measuring Gmax in the laboratory
‘Ping’ right
‘Ping’ left

## Slide 5: Fraser River Sand
Has laboratory test bender elements
Good range of soil density
Benders measuring during triaxial test (so shows “strain dependent elasticity – or lack thereof!)

## Slide 6: Fraser River Sand Benders
Bender elements were used with 7 triaxial tests
  2 bender tests were on “crushed” FRS
  Measurements taken during both consolidation and shearing stages
Fitted equation of the form
….to the shearing portion of the uncrushed triaxials.
where A, emin and b are fitted soil properties
pref is 100 kPa (or equivalent in same units as p)

## Slide 7: Goodness of fit – fitting data shown

## Slide 8: Elasticity - fit
A = 375
emin = 0.344
b = 0.466

## Slide 9: Elasticity – simpler equation for workshop
For simplicity the workshop spreadsheet adopts the simpler (but less accurate) equation:
…where a and b are fitted parameters, pref = 100 kPa.
Typically use this simpler equation (without void ratio) because if subsequently applying to field conditions you’ll likely not know in situ void ratio.

## Slide 10: Elasticity – simpler equation for workshop

## Slide 11: Elasticity – simpler equation for workshop
dense & compact (CID & CIU)
loose (CID)

## Slide 12: No ‘strain dependent modulus’
The small Gmax changes measured are all caused by changing p in the test

## Slide 13: Now to Nerlerk Sand (much older data…)