## Slide 1: 8b. CPT – Quantitative evaluation: SAND
Mike Jefferies, PEng
Dr. Dawn Shuttle, PEng
January, 2015
Determining y insitu

## Slide 2: CPT resistance in uniform soil
Tip..
Friction..
PWP..

## Slide 3: Calibration chamber for the CPT in SAND
Esso Resources Canada, Dome Petroleum, Gulf Canada Resources
…see Book for complete set of world’s calibration chamber data

## Slide 4: Sorting out CPT “interpretation”
BASIC ISSUES
How stress level affects qc-Dr
How soil properties affect qc-Dr

## Slide 5: Getting y from the CPT Been et al (1987)
Q
Esso Resources Canada, Dome Petroleum, Gulf Canada Resources
State parameter, y
Stress-normalized CPT resistance, Q

## Slide 6: Sands calibrated to CPT
Hilton Mine Tailings (Harman, 1976)
Ottawa (Harman, 1976)
Reid Bedford (Lhuer, 1976)
Ticino (Baldi et al, 1982 & 1986; Golder, 1987)
Monterey (Tringale, 1983; Huntsman, 1985)
Erksak (Been et al, 1987)
Hoksund (Lunne, 1986; Baldi et al, 1986)
Chek Lap Kok (Shen & Lee, 1995)
West Kowloon (Shen & Lee, 1995)
Syncrude Tailings (Golder 1988, pbl 2006)
Yatesville silty sand (Brandon et al, 1990)

## Slide 7: Sands calibrated to CPT
Same equation for each sand, just with different k,m values

## Slide 8: Sladen’s intervention…

## Slide 9: At some point you have to do “the math”
Need large displacement computations
    ‘moving mesh’ convects work and this needs including in solution
    convection also depends on dilation
    Zienkiewicz FE book not correct
    Appears simple, but actually rather sophisticated numerics
Approach
    Verify numerical implementation against constant friction, constant dilation soil for which “semi” closed-form solutions exist
    Verify numerical implementation of NorSand against direct integration for laboratory element tests
    Combine two verified modules to compute CPT behaviour
How can a properly dimensionless framework be wrong ?

## Slide 10: Doing the “the math”
qc =CQ Plimit

## Slide 11: Cavity expansion

## Slide 12: Cavity expansion analogue…….
CPT

## Slide 13: Doing “the math”: cavity expansion
qc =CQ Plimit
Cavity displacement
Cavity pressure
Bishop, Mott & Hill (1945)

## Slide 14: Scaling factor and data scatter
I169
E139
CQ
Ir = Gmax/p’0
...Identical reported e0, p0

## Slide 15: Single sand: Q = k exp(- m y )

## Slide 16: Effect of Gmax on Ticino CPT calibration
y = - m ln(Q/k)
f( Gmax / p’)
“Variable exponent” normalizations of CPT data are attempting to approximate the effect of Gmax on the penetration resistance (and doing so badly)

## Slide 17: Generalization from Ticino to all CC sands
331 calibration tests
80% ± 0.04

## Slide 18: Site-specific CPT calibration
Cavity expansion of NorSand is a pretty good analogue to CPT penetration resistance in calibration chambers
Determine soil properties
    M, N, l10, c, H… reconstituted samples (judgment ?)
    Measure Gmax insitu
    And then there is K0… 0.7 in alluvial deposits ?
Use numerical method
    “widget”

## Slide 19: What is the Widget
Spherical idealization
  1-D (= radial)
Coded specifically for this particular geometry
  Efficient… Plimit
Needs geometry correction CCPT
  Has been calibrated to true CPT geometry (from calibration chamber tests)
qc =CCPT Plimit

## Slide 20: Where is the Widget ?
Folder: /Data & Templates/ CPT programs/ CPTwidget/SandExample
Contains six files:
  CPTwidget_V2p5.exe
  CPTwidget.FIL
  SandExample.DAT
  SandExample.VAL
  WidgetSandExample_V2p5.xls
  SandExample_val.xls

## Slide 21: The Widget
CPTwidget_V2p5.exe
    Finite element spherical code
    Fortran – but being updated to C++
    Is set up to batch a series of CPT simulations
    “double click” to run
  CPTwidget.FIL
    Ascii text file
    Contains the root name of the simulations
    Your file contains the single word “SandExample”
    Do not change the name of this file

## Slide 22: The Widget
SandExample.DAT
    Ascii text file
    Contains:
      NorSand Calibration
      Mesh geometry
      Range of Simulations to run
        So if you need to stop the run you do not need to rerun from scratch
      Numerical tolerances

## Slide 23: SandExample.DAT
    Soil Model - 1=NorSand
    1
    NumNodes, MaxStrain(%), incU
    71 500 5.e-4
    toler, fmaxtol, tstepfac
    5.e-5 1.e-5 0.1
    Outer Radius
    250.
DO NOT ALTER
ALTER IF NEEDED
RARELY ALTER

## Slide 24: SandExample.DAT
Mtc Ntc lambda(log_e) Gamma(@1kPa) Pref Chi
1.45 0.43 0.06 1.22 1.0 4.85
H0 Hy
42 310
R (~ OCR)
1.00
Gpower Poisson
0.5 0.2
NorSand calibration:
(edit for other soils)

## Slide 25: Example1.DAT
PoreMod
0.0
istart istop
40
controls which simulations are run
Pore water modulus
Drained = 0., Undrained = 109 Pa

## Slide 26: SandExample.VAL
SandExample.VAL
    Ascii text file
    Contains the in situ conditions for the individual simulations
    Only 3 inputs
      p0 y0 Ir (= G0/p0)
    One row for each simulation
    To set up the .VAL file open in Excel and export as an Ascii file

## Slide 27: SandExample.VAL
Ir = 100
Ir = 250
Ir = 500
p0 = 100 kPa

## Slide 28: Run the CPTwidget
Find CPTwidget_V2p5.exe
“double click” to start
Edit CPTwidget.fil to contain SandExample
Now start the simulations !

## Slide 29: SandExample.OUT
SandExample.OUT contains the simulation results
Most easily explained by opening in Excel and plotting the results…..
Open and paste “space separated” into
“0 > raw data” sheet

## Slide 30: 0 > raw data
Not enough simulations complete, so stop the Widget running and open “one we prepared earlier” from handouts/CPTwidget/Results

## Slide 31: parametric_data_plot.xls
Open Widget_SandExample_V2p5.xls
Look at the “1> paste data from Widget” sheet headings
y0
Qp=(qt-p0)/p0’

## Slide 32: parametric_data_plot.xls

## Slide 33: Qp vs state

## Slide 34: Qp vs state
k = 24.65
m = 8.29

## Slide 35: Example results
Now open SandExample.OUT in Excel
Paste into the “0 > raw_data” sheet of WidgetSandExample_V2p5.xls
Copy over to the corresponding simulation range in “1>paste output from widget”
Review plotted results in “2 > fit trends”
Add exponential trend lines……
What are the values for m and k ?

## Slide 36: Example results
In the “2 > fit trends” sheet
For each Ir type in your derived k and m into the spreadsheet

## Slide 37: SandExample data

## Slide 38: Example results
View the k and m trend with Ir in the “3 > view calibration” sheet

## Slide 39: Back to our plotting program: CPTplot.xls
Interpretation Step 1: Input Gmax

## Slide 40: Representing Gmax for evaluating CPT data
Calcs use Gmax trend

## Slide 41: Choosing y method

## Slide 42: Options for y method in CPTplot.xls
Method 1: Specify k, m for use in drained part of sounding
    From assessment of calibration chamber data (eg Been et al, 1987)
    Use CPTwidget to compute k, m
Method 2: Specify soil properties for use in drained part of sounding
    Trends for k,m based on extensive parametric simulations
    Needs soil properties M, l, H…
Method 3: Specify k’, m’ for undrained part of sounding
    Use CPTwidget to compute k’, m’
Method 4: ‘Universal Method’ …always a background result
    Infers key soil properties from CPT every ~100 mm
    Minimal soil property input
Undrained if: |Bq| > 0.1 or F > 1%

## Slide 43: Method 1: drained soundings (effective stress)
Method Inputs
k, m
Options:
1a – use Widget
1b – chamber data

## Slide 44: Widget input to CPTplot

## Slide 45: Output from Method 1

## Slide 46: Method 2: Influence factors

## Slide 47: Input for Method 2

## Slide 48: Output for Method 2